CUBIX CX 5212

Manufacturer: RIM CZ a.s.

Design: Kai Stania

CUBIX CX 5212

Exclusive collection of sofas and armchairs suitable for office areas with modern and airy design of cubic shapes.

The collection includes single to three-seater segments on metal frame. These segments can be used as workplace for relax areas or as a place for informal meeting and relaxing gathering.

| Design | The structure is made of squared spruce timbers and chipboard and built on a metal support frame. PUR foam is glued on the individual parts of structure and cut to desired shapes. The seating part is made of wooden frame with zig-zag springs providing higher seating comfort. The seat is equipped with high quality PUR foam with 120 mm thickness, bulk weight 50 kg/m3. The seating part is 440 mm high. Two types of armrests, lower 200 mm, higher 300 mm. As for individual segments (seating part without backrest and armrests), the aluminium supporting frame is replaced with a solid wood structure and seat is without zig-zag springs. Type and thickness of foam are identical to sofas variant. |
| --- | --- |
| Frame | The supporting frame is welded from metal profiles 50x30x2mm and L-profile 30x30x2mm, painted with black powder coating and fixed to the wooden structure. The corner legs are firmly attached to the supporting frame and connected with 25x2mm tubes with chrome surface treatments. |
| Feet | An aluminium corner foot with adjustable chrome glide. Polished aluminium surface treatment. |
| Upholstery | To be selected from fabric collection. |
| Options | Feet and tubes surface treatment – powder coating as per RAL. |
| Warranty | 5 years (see Business conditions). |
| Variants | CX 5210 upholstered single-seater segment CX 5220 upholstered two-seater segment CX 5230 upholstered three-seater segment CX 5211 upholstered single-seater armchair with low armrest CX 5212 upholstered two-seater armchair with low armrest CX 5213 upholstered three-seater armchair with low armrest CX 5212 upholstered single-seater armchair with high armrest CX 5222 upholstered two-seater armchair with high armrest CX 5232 upholstered three-seater armchair with high armrest |

Dimensions (in mm)

Variants IX

| CX 5211 |  |
| --- | --- |
| CX 5221 |  |
| CX 5231 |  |
| CX 5222 |  |

TABLES

| Design | Standard table structure is made of black or white lacquered MDF, with 6 mm thick glass painted from the underside (black or white colour). |
| --- | --- |
| Frame | The frame consists of aluminium corner foot and tubes of Ø25x2mm. Chrome surface treatment of tubes. |
| Feet | An aluminium corner foot with adjustable chrome glide. Polished aluminium surface treatment. |
| Options | Feet and tubes surface treatment: black powder coating as per RAL. |
| Warranty | 5 years (see Business conditions). |
| CX 5251 |  |
| CX 5252 |  |